
|  |  |
| --- | --- |
| HBC | 金属化聚酯薄膜交流用电容器 |
|  |
| **Metallized** **Polyester** **Film** **Capacitor(VAC)-** CL21(VAC) |



**FEATURES**

►Non-inductive, coated with epoxy resin or flame retardant epoxy power.

►High capacitance stability.

►High moisture resistance

►High reliability with self-healing performance.

►Recommendable for high frequency circuit use.

►Possibility production of special specification.

►Competitive price.

**SPECIFICATIONS**

|  |  |
| --- | --- |
| Temperature Range | -40℃~+105℃ |
| Rated Voltage | 250VAC/275VAC/300VAC/400VAC |
| Capacitance Range | 0.01～1.5 μF |
| Capacitance Tolerance | ±5%,±10%,±20% |
| Insulation Resistance | 2,000MΩ |
| Dissipation Factor | 1% max.(at1KHz) |
| Dielectric Strength | 175% of rated voltage for 5 sec. |

.

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **STANDARD** **SIZE(mm)** | | | | | |
| **VAC**  **Mfd** | **L** | **H** | **T** | **P** | **d** |
| **0.01** | 13 | 8.5 | 4.2 | 10 | 0.6 |
| **0.015** | 13 | 8.8 | 4.8 | 10 | 0.6 |
| **0.018** | 13 | 9.3 | 5 | 10 | 0.6 |
| **0.022** | 13 | 9.5 | 5.8 | 10 | 0.6 |
| **0.027** | 13 | 8.7 | 5.3 | 10 | 0.6 |
| **0.033** | 13  18 | 9 | 5.8  5.2 | 10  15 | 0.6  0.8 |
| 9 |
| **0.039** | 13 | 9 | 5 | 10 | 0.6 |
| 18 | 9.5 | 6 | 15 | 0.8 |
| **0.047** | 13 | 9.5 | 5.5 | 10 | 0.6 |
| 18 | 10 | 6.5 | 15 | 0.8 |
| **0.056** | 13 | 10.5 | 6 | 10 | 0.6 |
| 18 | 11.5 | 6 | 15 | 0.8 |
| **0.068** | 13 | 11.4 | 6 | 10 | 0.6 |
| 18 | 10.5 | 6 | 15 | 0.8 |
| **0.082** | 13 | 11 | 6.2 | 10 | 0.6 |
| **0.1** | 13 | 11.8 | 7 | 10 | 0.6 |
| 18 | 10.5 | 5.8 | 15 | 0.8 |
| **0.15** | 13 | 13.5 | 8 | 10 | 0.6 |
| 18 | 12.5 | 6.5 | 15 | 0.8 |
| **0.18** | 18 | 13 | 7.0 | 15 | 0.8 |
| **0.22** | 18 | 14.5 | 7.5 | 15 | 0.8 |
| **0.27** | 18 | 13.5 | 7.6 | 15 | 0.8 |
| **0.33** | 18 | 14 | 8 | 15 | 0.8 |
| **0.39** | 23 | 14.8 | 9 | 20 | 0.8 |
| **0.47** | 23 | 16 | 9.8 | 20 | 0.8 |
| **0.56** | 23 | 18 | 10 | 20 | 0.8 |
| **0.68** | 23 | 19.5 | 11 | 20 | 0.8 |
| **0.82** | 23 | 21 | 11.5 | 20 | 0.8 |
| **1.0** | 25 | 21.5 | 12 | 22 | 0.8 |
| **1.5** | 31 | 23.5 | 13 | 27 | 0.8 |

**Please visit our website to get more update data, those data & specification are subject to change without notice.**

|  |  |  |
| --- | --- | --- |
| **Shantou Xin Hua Xiong Electronios Industry Co.,Ltd.** | | |
| **www.cn-huaxiong.com** | **Tel:【+86】0754-87727171** | **QQ :2851010898** |
| **E-mail:133269599@qq.com** | **Fax:【+86】 0754-87728582** | **whatsapp:86+15502000092** |

